**Electrolytic Plating Solution - 7 Gallons**

(NOTE: This will fill the Electrolytic plating system and give around 1/2 gallon to spare)

7 Gallons - Distilled Water

9.33 lbs - Copper Sulfate (Zep Root Killer)

7oz - Copper Brightener A ([Caswellplating.com](http://Caswellplating.com))

18.67oz - Copper Brightener B ([Caswellplating.com](http://Caswellplating.com))

4 lbs - Borax (20 Mule Team)

93.3oz (9 1/3 cups) - Sulfuric Acid (Battery Acid at Auto Store)